Textiles — Duvet and Duvet covers —Specification

Contents	Page

Foreword	iv

1	Scope	1

2	Normative references	1

3	Terms and definitions	2

4	Requirements	3

4.1	General requirements	3

4.2	Specific requirements	3

4.2.1	Fibre composition of the casing fabric and filling	3

4.2.2	Dimensions	3

4.2.3	Seams and stitching	3

4.2.4	Warmth-to-mass ratio	3

4.2.5	Mass per unit area	3

4.2.6	Thermal insulance	3

4.2.7	Permeability of casing fabrics	3

4.2.8	Physical properties of casing fabrics	4

4.2.9	Colour fastness properties of casing fabrics	4

4.2.10	Restricted colourants	5

5	Packaging	5

6	Labelling	5

7	Sampling	5

Annex A (normative)  Determination of thermal insulance	6

A.1	Apparatus	6

A.2	Procedure	6

Annex B (normative)  Determination of mass per unit area	8

Annex C (normative)  Determination of warmth-to-mass ratio	9

Bibliography	10

12

#### Foreword

The African Organization for Standardization (ARSO) is an African intergovernmental organization established by the United Nations Economic Commission for Africa (UNECA) and the Organization of African Unity (AU) in 1977. One of the fundamental mandates of ARSO is to develop and harmonize African Standards (ARS) for the purpose of enhancing Africa’s internal trading capacity, increase Africa’s product and service competitiveness globally and uplift the welfare of African communities. The work of preparing African Standards is normally carried out through ARSO technical committees. Each Member State interested in a subject for which a technical committee has been established has the right to be represented on that committee. International organizations, Regional Economic Communities (RECs), governmental and non-governmental organizations, in liaison with ARSO, also take part in the work.

ARSO Standards are drafted in accordance with the rules given in the ISO/IEC Directives, Part 2.

The main task of technical committees is to prepare ARSO Standards. Draft ARSO Standards adopted by the technical committees are circulated to the member bodies for voting. Publication as an ARSO Standard requires approval by at least 75 % of the member bodies casting a vote.

Attention is drawn to the possibility that some of the elements of this document may be the subject of patent rights. ARSO shall not be held responsible for identifying any or all such patent rights.

This African Standard was prepared by the ARSO/TC 53, Textiles, textile products and accessories.

© African Organisation for Standardisation 2026 — All rights reserved*

ARSO Central Secretariat

International House 3rd Floor

P. O. Box 57363 — 00200 City Square

NAIROBI, KENYA

Tel. +254-20-2224561, +254-20-3311641, +254-20-3311608

E-mail: arso@arso-oran.org

Web: www.arso-oran.org

Copyright notice This ARSO document is copyright-protected by ARSO. While the reproduction of this document by participants in the ARSO standards development process is permitted without prior permission from ARSO, neither this document nor any extract from it may be reproduced, stored or transmitted in any form for any other purpose without prior written permission from ARSO. Requests for permission to reproduce this document for the purpose of selling it should be addressed as shown below or to ARSO’s member body in the country of the requester: © African Organisation for Standardisation 2026 — All rights reserved ARSO Central Secretariat International House 3rd Floor P.O. Box 57363 — 00200 City Square NAIROBI, KENYA Tel: +254-20-2224561, +254-20-3311641, +254-20-3311608 E-mail: arso@arso-oran.org Web: www.arso-oran.org Reproduction for sales purposes may be subject to royalty payments or a licensing agreement. Violators may be prosecuted.

AFRICAN STANDARD 	 DARS 1597:2026

Textiles — Duvets and Duvet covers — Specification

- Scope

This Draft African Standard specifies requirements, sampling, and test methods for duvets and duvet covers

## 2	Normative references

The following documents are referred to in the text in such a way that some or all of their content constitutes requirements of this document. For dated references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies.

ISO 105-B01, Textiles — Tests for colour fastness — Part B01: Colour fastness to light: Daylight

ISO 105-B02, Textiles — Tests for colour fastness — Part B02: Colour fastness to artificial light: Xenon arc fading lamp test

ISO 105-C10, Textiles — Tests for colour fastness — Part C10: Colour fastness to washing with soap or soap and soda

ISO 105-D01, Textiles — Tests for colour fastness — Part D01: Colour fastness to drycleaning using perchloroethylene solvent

ISO 105-E04, Textiles — Tests for colour fastness — Part E04: Colour fastness to perspiration

ISO 105-X12, Textiles — Tests for colour fastness — Part X12: Colour fastness to rubbing

ISO 139, Textiles — Standard atmospheres for conditioning and testing

ISO 1833 (all parts), Textiles — Quantitative chemical analysis

ISO 3175-1, Textiles — Professional care, drycleaning and wetcleaning of fabrics and garments — Part 1: Assessment of performance after cleaning and finishing

ISO 3758, Textiles — Care labelling code using symbols

ISO 3759, Textiles — Preparation, marking and measuring of fabric specimens and garments in tests for determination of dimensional change

ISO 5077, Textiles — Determination of dimensional change in washing and drying

ISO 6330, Textiles — Domestic washing and drying procedures for textile testing

ISO 8498, Woven fabrics — Description of defects — Vocabulary

ISO 8499, Knitted fabrics — Description of defects — Vocabulary

ISO 9237, Textiles — Determination of the permeability of fabrics to air

ISO 12945-2, Textiles — Determination of fabric propensity to surface pilling, fuzzing or matting — Part 2: Modified Martindale method

ISO 13934-1, Textiles — Tensile properties of fabrics — Part 1: Determination of maximum force and elongation at maximum force using the strip method

ISO 13938-2, Textiles — Bursting properties of fabrics — Part 2: Pneumatic method for determination of bursting strength and bursting distension

ISO 14362-1, Textiles — Methods for determination of certain aromatic amines derived from azo colorants — Part 1: Detection of the use of certain azo colorants accessible with and without extracting the fibres

ISO 14362-3, Textiles — Methods for determination of certain aromatic amines derived from azo colorants — Part 3: Detection of the use of certain azo colorants, which may release 4-aminoazobenzene

ISO 16373-1, Textiles — Dyestuffs — Part 1: General principles of testing coloured textiles for dyestuff identification

ISO 16373-2, Textiles — Dyestuffs — Part 2: General method for the determination of extractable dyestuffs including allergenic and carcinogenic dyestuffs (method using pyridine-water)

ISO 16373-3, Textiles — Dyestuffs — Part 3: Method for determination of certain carcinogenic dyestuffs (method using triethylamine/methanol)

ISO 22198, Textiles — Fabrics — Determination of width and length

ISO 24153, Random sampling and randomization procedures

# 3	Terms and definitions

For the purposes of this document, the following terms and definitions apply.

ISO and IEC maintain terminological databases for use in standardization at the following addresses:

— ISO Online browsing platform: available at http://www.iso.org/obp

3.1

duvet

bed covering, consisting of insulating filler secured between two layers of fabric designed to reduce heat loss

3.2

warmth-to-mass ratio

measure of the efficiency of the duvet which equals to the ratio of the thermal resistance of the duvet (in togs) to its mass per unit area

3.3

tog value

unit equal to ten times the thermal insulance

Note1 to entry:	Tog is also known as thermal resistance of a duvet.

3.4

duvet covers

is a protective, removable fabric case that encloses a duvet insert

Note1 to entry:	Tog is also known as thermal resistance of a duvet.

# 4	Requirements

## 4.1	General requirements

    - Duvets and duvet covers shall be:

- free from defects that could affect their appearance or their performance (or both);

- made from material that do not contain harmful substances

- made such that all seams are neatly stitched and securely backstitched, free from twists, pleats and puckers, and sufficiently extensible to prevent seam-cracking and undue shrinkage in use, made such that all ends of sewing threads have been trimmed and loose threads removed;

- filling material shall be evenly distributed to remain in the same position during normal use and care for duvet

- cleaned in accordance with the care instructions, without giving rise to any defect; such as puckering, lumpiness, tears, etc

    - The ends and side edges shall be secured together by seaming, binding, or overlocking.

    - Shall be constructed to allow for easy insertion and removal without damage.

## 4.2	Specific requirements

### 4.2.1	Fibre composition of the casing fabric and duvet cover

The fibre composition and proportion shall be as declared when tested in accordance with any relevant part of ISO 1833. Where the fabric is a blend of two or more fibres, the fibre composition and proportion shall be as declared, subject to a tolerance of ± 3 %.

### 4.2.2	Dimensions

The mean width and mean length of duvets and duvet cover shall not vary by more than ± 5 % from the dimensions declared on the label when measured in accordance with ISO 22198.

### 4.2.3	Seams and stitching

All seams of the casing shall be sewn with not less than 32 stitches per 10 cm for duvets, unless one of the following occurs:

- if the edges of the casing are bound in this case, they shall be sewn with not less than 20 stitches per 10 cm; and

- if the edges of the casing are overlocked in this case, they shall be sewn with not less than 50 stitches per 10 cm.

### 4.2.4	Thermal insulance

When determined in accordance with Annex A the thermal insulance of a duvet shall be within -0.5 togs or +3 togs of the declared value.

### 4.2.5	Mass per unit area

The mass per unit area shall be within ±5 % of the declared value when measured in accordance with Annex B.

### 4.2.6	Warmth-to-mass ratio

When determined in accordance with Annex C, the warmth-to-mass ratio of a duvet shall be at least 100.

The recommended TOG value is indicated in Annex D

### 4.2.7	Permeability of casing fabrics

The casing fabric shall be capable of satisfactorily retaining the filling and allowing a sufficient level of moisture vapour transmission.

### 4.2.8	Physical properties of casing fabrics

Duvets shall comply with the physical requirements given in Table 1 when tested in accordance with the test methods specified therein.

Table 1 — Physical requirements for casing fabric for duvets and duvet cover

| S/N | Parameter |  | Requirement |  | Test method |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Woven casing fabric | Knitted casing fabric |  |
|  | Breaking strength, N, min. | Warp | 350 | N/A | ISO 13934-1 |
|  |  | Weft | 200 | N/A |  |
|  | Bursting strength, kpa, min. |  | N/A | 155 | ISO 13938-2 |
|  | Pilling, min. |  | 4 | 4 | ISO 12945-2 |
|  | Dimensional changes after five washes, % |  | ±3 | ±5 | ISO 6330 (Procedure 4N), ISO 5077 and ISO 3759 |
|  | Dimensional changes after five dry cleaning cycles, % |  | ±3 | ±5 | ISO 3175-1 |
|  | Air permeability, ml/(cm2.s) | Woven casing made from spun staple yarns | 25 - 30 | - | ISO 9237 |
|  |  | Casing made from other woven fabrics | 15 - 20 | - |  |

### 4.2.9	Colour fastness properties of duvet casing fabrics and duvet covers

Duvets and duvet covers shall comply with the colour fastness requirements given in Table 2 when tested in accordance with the test methods specified therein.

Table 2 — Colour fastness requirements for duvet casing fabric and covers

| S/N | Parameter |  | Requirement |  | Test method |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Woven duvet | Knitted duvet |  |
|  | Colour fastness to washing, min. | Colour change | 4 | 4 | ISO 105-C10 |
|  |  | Staining |  |  |  |
|  | Colour fastness to dry cleaning, min. | Colour change | 4 | 4 | ISO 105-D01 |
|  |  | Staining |  |  |  |
|  | Colour fastness to rubbing, min. | Dry | 4 | 4 | ISO 105-X12 |
|  |  | Wet | 3-4 | 3-4 |  |
|  | Colour fastness to light, min. |  | 4 | 4 | ISO 105-B02, ISO 105-B01 |
|  | Colour fastness to perspiration (acid), min. | Colour change | 4 | 4 | ISO 105-E04 |
|  |  | Staining |  |  |  |
|  | Colour fastness to perspiration (alkali), min. | Colour change | 4 | 4 |  |
|  |  | Staining |  |  |  |

### 4.2.10	Restricted colourants

The printed casing fabric for duvets and duvet cover shall not contain any of the banned dyestuffs listed in Annex E and azo dyestuffs/pigments which release any of the carbylamines given in Annex F when tested in accordance with ISO 14362-1, ISO 14362-3, ISO 16373-2 and ISO 16373-3.

# 5	Packaging

5.1 Duvets and duvet covers shall be wrapped individually in a suitable wrapper and packed in a suitable bulk container.

5.2 Packaging shall protect the products from contamination, moisture, and damage during storage and transportation

# 6	Labelling

The following information shall appear, in legible and indelible marking on a label securely attached to an edge of, or on top (near one of the corners) of each duvet and duvet cover:

- manufacturer’s name or trademark;

- length and width in centimetres;

- fibre composition of the casing fabric and of the filling;

- care instructions in accordance with ISO 3758;

- tog value;

- mass per unit area, in g/m2; and

- country of manufacture.

# 7	Sampling

Sampling shall be done in accordance with ISO 24153.

Annex A
(normative)

Determination of thermal insulance

## A.1	Apparatus

A.1.1	Electric blanket, of size at least 600 mm × 450 mm, that has electricity supplies controlled by a variable transformer or that has a set-point controller.

A.1.2	Polyurethane foam mattress, of a nominal thickness 25 mm and of a length and width greater than the corresponding dimensions of the duvet under test.

A.1.3	Aluminum sheet, of thickness 1.5 mm and of other dimensions equal to those of the electrically heated blanket.

A.1.4	Two pieces of a polyester-and-cotton shirting, each of length and width slightly greater than the corresponding dimensions of the duvet under test.

A.1.5	At least six thermocouples.

A.1.6	At least six small low-temperature heat flow meters.

A.1.7	Adhesive tape.

A.1.8	Suitable slow-speed fan, capable of creating a horizontal breeze of velocity not exceeding 0.3 m/s over the entire upper surface of the duvet.

## A.2	Procedure

A.2.1	Determine, to the nearest 1 g, the mass of the duvet under test and record the mass in kilograms.

A.2.2	Place the mattress on a table and place the electric blanket in the centre of the mattress.

A.2.3	Cover the electric blanket with the aluminium sheet, and then cover the latter with one of the pieces of fabric.

A.2.4	Within an area of size 450 mm × 350 mm and within the boundaries of the electric blanket, tape the heat flow meters and the thermocouples to the upper surface of the piece of fabric in random configuration.

A.2.5	Gently place the duvet over the entire assembly and ensure that no heat flow meter is closer than 300 mm to an edge or end of the duvet, and cover with the other piece of fabric.

A.2.6	Place the fan in such a position that it creates a horizontal breeze of velocity not exceeding 0.3 m/s over the entire upper surface of the duvet.

A.2.7	Suspend two more thermocouples 300 mm above the assembly and in the air stream created by the fan.

A.2.8	Switch on the electric blanket and so adjust the power supply that the temperature under the duvet is maintained at 33 °C ± 5 °C.

A.2.9	Record the temperature indicated by each thermocouple and the rate of heat flow indicated by each heat flow meter disc. Calculate the mean ambient temperature (as indicated by the suspended thermocouples), the mean temperature under the duvet, and the rate of heat flow.

A.2.10	Calculate the thermal insulance, using the formula below:

M=(t1-t2)Ø

where

M	is the thermal insulance, in metre-squared kelvin per watt, of the duvet;

t1	is the mean temperature under the duvet, in degrees Celsius;

t2	is the mean ambient (room) temperature, in degrees Celsius;

ø	is the mean rate of heat flow, in watts per square metre.

A.2.11	Select two additional test areas by moving the duvet plus the upper piece of fabric, ensuring that the test areas do not overlap, and on each of these areas repeat the procedures given in A.2.9 and A.2.10.

A.2.12	From the results on the three test areas, calculate the mean thermal insulance of the duvet plus the cover fabric.

A.2.13	Remove the duvet and repeat the procedures given in A.2.9 and A.2.10 with the upper piece of fabric as the only means for covering the assembly.

A.2.14	Calculate the mean thermal insulance of the upper piece of fabric.

A.2.15	Calculate the total mean thermal insulance of the duvet by subtracting the value obtained in A.2.14 from the value obtained in A.2.12.

A.2.16	Calculate the tog value by multiplying the thermal insulance (A.2.15) by ten.

A.2.17	Check for compliance with 4.2.6.

Annex B
(normative)

Determination of mass per unit area

B.1	Condition the duvet in accordance with ISO 139.

B.2	Determine the mass of the conditioned duvet to the nearest gram.

B.3	Calculate the mass per square metre using the formula below:

Mass per square metre=104×m(b×l)

where

m	is the mass, in grams, of the conditioned duvet;

b	is the width, in centimetres, of the duvet, determined in accordance with ISO 22198; and

l	is the length, in centimetres, of the duvet, determined in accordance with ISO 22198.

B.4	Express the results in grams per square metre (g/m2).

Annex C
(normative)

Determination of the warmth-to-mass ratio

C.1.1	Determine, to the nearest centimetre, the length and width (see 4.2.2) of the duvet.

C.1.2	Calculate the mean length and the mean width of the duvet in meters.

C.1.3	Calculate the warmth-to-mass ratio, Q, in meters to the fourth kelvin per watt per kilogram, using the formula below:

Q=(M×l×b)m×10

where

M	is the mean thermal insulance (see A.2.15), in metre-squared kelvin per watt, of the duvet;

l	is the mean length (see C.1.2), in metres, of the duvet;

b	is the mean width (see C.1.2), in metres, of the duvet; and

m	is the mass, in kilograms, of the duvet (see A.2.1).

Annex D
(Informative)

Recommended TOG ratings by night temperature

| Night Temperature Range | Recommended TOG | Duvet Classification | Comfort Level | Best For |
| --- | --- | --- | --- | --- |
| -5°C to 5°C | 10.0 - 13.5 TOG | Winter / Heavy Weight | Maximum warmth | Very cold nights, frost conditions, unheated rooms |
| 5°C to 15°C | 7.0 - 10.5 TOG | Spring/Autumn / Medium Weight | Moderate warmth | Cool to mild nights, transitional seasons |
| 15°C to 25°C | 3.0 - 4.5 TOG | Summer / Light Weight | Light covering | Warm nights, heated rooms, tropical climates |

Annex E

(Normative)

List of Banned Dyestuffs

Table E.1 – Banned Dyestuffs

| No. | Generic Name | C.1 Structure No. C.1 Constitution No. | Chemical class |
| --- | --- | --- | --- |
| 1 | C.1 Acid red 26 | 16150 | Monoazo |
| 2 | C.1 Basic red 9 | 42500 | Triarylamine |
| 3 | C.1 Basic violet 14 | 42510 | Triarymethane |
| 4 | C.1 Direct black 38 | 30335 | Triazo |
| 5 | C.1 Direct blue 6 | 22610 | Diazo |
| 6 | C.1 Direct red 28 | 22120 | Diazo |
| 7 | C.1 Disperse blue 1 | 64500 | Anthraquinone |
| 8 | C.1 Disperse orange I I | 60700 | Anthraquinone |
| 9 | C.1 Disperse blue 3 | 61505 | Anthraquinone |
| 10 | C.1 Disperse blue 7 | 62500 | Anthraquinone |
| 11 | C.1 Disperse blue 26 | 63305 | Anthraquinone |
| 12 | C.1 Disperse blue 35 | - | Anthraquinone |
| 13 | C.1 Disperse blue 102 | - | Monoazo |
| 14 | C.1 Disperse blue 106 | - | Azo |
| 15 | C.1 Disperse blue 124 | - | Monoazo |
| 16 | C.1 Disperse yellow 1 | 10345 | Nitro |
| 17 | C.1 Disperse yellow 3 | 11855 | Azo |
| 18 | C.1 Disperse yellow 9 | 10375 | Nitro |
| 19 | C.1 Disperse yellow 39 | - | - |
| 20 | C.1 Disperse yellow 49 | - | Methine |
| 21 | C.1 Disperse orange 1 | 11080 | Azo |
| 22 | C.1 Disperse orange 3 | 11005 | Azo |
| 23 | C.1 Disperse orange 37 | - | Monoazo |
| 24 | C.1 Disperse orange 76 | - | Monoazo |
| 25 | C.1 Disperse red I | 11110 | Monoazo |
| 26 | C.1 Disperse red II | 62015 | Anthraquinone |
| 27 | C.1 Disperse red 17 | 11210 | Monoazo |
| 28 | C.1 Disperse brown I | 11152 | Monoazo |

Annex F

(Normative)

List of Banned Dyestuffs

Table F1-Arylamines cleaved from azo dyestuffs and pigments

| No | Amine |
| --- | --- |
| 1 | 4 – aminodiphenyl |
| 2 | Bendizine |
| 3 | 4 – chloro-o-toluidine |
| 4 | o-aminoazotoluene |
| 5 | p-choroaniline |
| 6 | 2.4 – diaminoanisole |
| 7 | 4.4 – diaminodiphenylmethane |
| 8 | 3.3’ – dichlorobenzidine |
| 9 | 3.3’ – dimethaxybenzidine |
| 10 | 3.3’ – dimethylbenzidine |
| 11 | 3.3’ – dimethyl -4,4’- diaminodiphenylmethane |
| 12 | p- cresidine |
| 13 | 4.4’ – methylene-bis-( 2-chloroaniline) |
| 14 | 4.4’ – oxidianiline |
| 15 | 4.4’ – thiodianiline |
| 16 | 4.4’ – thiodianiline |
| 17 | o- toluidine |
| 18 | 2.4’ toluylendiamine |
| 19 | 2.4.5’ trimethylaniline |
| 20 | o-anisidine |
| 21 | 2.4 – xylidine |
| 22 | 2.6 – xylidine |
| 23 | 4 - - aminoazobenzene* |
| 24 | 2 – naphthylamine |
| 25 | 2 – amino-4-nitrofoluene |

*No validated test method exists for this amino yet

Annex G
(Informative)
Fillings

G.1 Plumage filling

A plumage filling should comply with the following relevant requirements

G.1.1 Down fibre or feather fibre content (or both)

The down fibre or feather fibre content (or both) of a plumage filling should not exceed 8 % (m/m) in a landfowl or waterfowl feather filling and 5 % (m/m) in any of the other three types of filling (see A.1.3).

NOTE - The composition of feathers in a waterfowl filling should be as follows:

Waterfowl feathers, % (m/m), min.	90

Landfowl feathers, % (m/m), max.	10

G.1.2 Residual matter

The residual matter of a plumage filling should not exceed 2 % (m/m).

G.1.3 Filling power index is power filling index a formal or standard term used in textiles?

The filling power index determined in accordance with the plumage filling should be at least equal to the appropriate of the following:

| Type of filling | Filling power index, min. |
| --- | --- |
| Down Down and feathers Feathers and down Waterfowl feathers Landfowl feathers | 75 60 50 45 – |

G.2 Synthetic-fibre filling

A synthetic-fibre filling should consist entirely of clean, crimped continuous filaments or staple synthetic fibres, of (in both cases) linear density between 4,5 dtex and 17,0 dtex . The length of staple fibres should be at least 30 mm. The fibres should be thermos-bonded or resin-bonded and the blend of melting fibres should not exceed 30 %.

The mass per unit area of the filling including, when relevant, the surface stabilizer, should be:

a)	150 g/m2 minimum. ("summer weight"); and

Annex H
(Informative)

Dimensions

Table 1  - Guideline on the finished dimensions for duvets

| 1 | 2 | 3 |
| --- | --- | --- |
| Bed size | Dimensions |  |
|  | cm |  |
|  | Width | Length |
| Single Three-quarter Double | 130-140 150 200 | 200 200 200 |
| Queen King Extra king | 230 230 250 | 200 220 220 |

Bibliography

FDKS 2668: 2016, Duvet, quilts and accessory products — Specification

* 2026 ARSO — All rights of exploitation reserved worldwide for African Member States’ NSBs.